## Slide 1: New integral experiments in Rez
Michal Kostal, LR-0 reactor lab, Rez
"Consultancy Meeting of the International Nuclear Data Evaluation Network (INDEN) on the Evaluated Data of Structural Materials„
Vienna, December 18th - 21th 2023

## Slide 2: Research infrastructure used by CVR group in new experiments
3 research reactors LR-0, LVR-15, VR-1 (university)
252Cf neutron sources
  Material blocks for neutron leakage measurements:
    spheres (Fe, Ni … and others)
    cubes (stainless steel, Cu, graphite)
  Spherical tank with aqueous solutions for prompt gamma leakage measurements
    NaCl, MnSO4, FeSO4, …. , planned CO(NH2)2 (ad blue) , and many others
DT generators
Well-described AmBe
XRF analyzers
(and many others)
2

## Slide 3: Neutron spectrometry
Well characterized spectrometer
Validation in PTB
Validation in 252Cf
Verified in Si filtered spectrum
Radulovic et al., IAEA, INDC(NDS)-0746, 2018
Chart: 6.8 MeV
Chart: Energy [MeV]
 | 0 | 0
Chart: Energy [MeV]

## Slide 4: Gamma spectrometry - HPGe
Most important is detector sensitivity
Foil measurement
  Mathematical model allows even large samples on detector cap
  Determination of coincidence summing correction
Gamma flux measurement
  Model allows evaluation of gamma flux (only the directionality needed)
Czakoj et al., Rad. Phys. and Chem. 202 (2023) 110542
Chart: Energy [MeV]
| 5.8999999999999997E-2 | 1.8360000000000001
 | 0 | 0
End cap geometry | -0.010778 | 0.0017983 | 0.0085654 | 0.036665 | -0.022369 | 0.0099755 | 0.0081456 | 0.022685 | 0.022186 | -0.020488
Marinelli beaker geometry | 0.0044822 | -0.012805 | -0.007247 | -0.0084622
Chart: Energy [MeV]
| 6.0399999999999995E-2 | 0.66166999999999998 | 1.17319 | 1.33253
Volume source | -0.019779 | -0.034436 | 0.010251 | 0.015024
In axis geometry | -0.010907 | 0.027575 | 0.0095603 | -0.009843 | -0.0098427
Perpendicular geometry | -0.00068257 | 0.0086285 | -0.0030522 | -0.010483 | -0.0034002
Chart: Energy [keV]
| 59.540900000000001 | 122.06055000000001 | 136.47355999999999 | 391.69799999999998 | 661.65700000000004 | 898.04200000000003 | 1173.2280000000001 | 1332.492 | 1836.0360000000001
Experiment | 0.025276 | 0.15989 | 0.16466 | 0.08292 | 0.05346 | 0.04135 | 0.03239 | 0.029503 | 0.024243
MCNP verified model | 0.016552 | 0.15391 | 0.1609 | 0.083948 | 0.052926 | 0.041101 | 0.03314 | 0.029787 | 0.022585
MCNP data sheet | 0.094873 | 0.23609 | 0.23514 | 0.11246 | 0.07116 | 0.055373 | 0.044684 | 0.040151 | 0.030561
MCNP radiogram | 0.091889 | 0.22313 | 0.22088 | 0.10123 | 0.063363 | 0.049035 | 0.039428 | 0.035414 | 0.026783

## Slide 5
Gamma spectrometry stilbene
Chart: E [MeV]
Chart: E [MeV]
| 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4
Simulation | 0.020503 | 0.018066 | 0.016958 | 0.015936 | 0.015497 | 0.015449 | 0.01562 | 0.016321 | 0.018013 | 0.022306 | 0.019719 | 0.0077228 | 0.004375 | 0.0041393 | 0.004135 | 0.004451 | 0.0049623 | 0.0043874 | 0.0045235 | 0.0047617 | 0.0050209 | 0.0056229 | 0.006716 | 0.0072982 | 0.0044353 | 0.0012245 | 0.0001619 | 1.42e-05 | 4.1e-06 | 3.1e-06 | 2.9e-06 | 2.8e-06 | 3.1e-06 | 2.4e-06 | 2e-06 | 2.1e-06 | 5e-07 | 4e-07 | 0
Newly developed response matrix
Simulation uses precise probe parameters
  In gamma transport surrounding materials are essential
Validation in AmBe + 24Na
Chart: Energy [MeV]

## Slide 6: Benchmarking (stainless steel (A-320) )
Chart: Channel
Fe | 0.6783
Cr | 0.1965
Ni | 0.0925
Mn | 0.0180
Mo | 0.00403
Si | 0.00344
Cu | 0.00343
Ti | 0.00267
V | 0.000563
Sn | 0.000131
Good separation in metallic benchmarks – cut at ~ 0.8 MeV
6
Relatively low background
Integral experiments are suitable for tuning of evaluations due to „low“ uncertainties
The leakage experiments with 252Cf(s.f) are ideal for validations due to low source uncertainties
Even in fusion, lower energies are essential to cover the slowing down process

## Slide 7: Benchmarking in 2023
ALARM-CF-NI-SHIELD-001 “Neutron Activation Foils and Fast Neutron Leakage Spectra from Nickel Sphere with 252Cf Source in the Center”
ALARM-CF-FE-SHIELD-002 “Neutron Activation Foils and Fast Neutron Leakage Spectra from Iron Sphere with 252Cf Source in the Center”
ALARM-CF-SST-SHIELD-001 “Neutron Activation Foils and Fast Neutron Leakage Spectra from a Stainless Steel 321 Block with a 252Cf Source in the Center.”
Chart: Energy [MeV]
Chart: Energy [MeV]
Chart: Energy [MeV]
Fe D=50
Ni D=50
A 320 50x50x50cm

## Slide 8: Gamma spectra from solution
PMMA sphere (o. d. 70 cm) filled with water with dissolved
  NaCl
  FeSO4
  MnSO4
HPGe + stilbene measurement
HPGe with HDPE + Cd shield
252Cf neutron source
 | a | b
NaCl | 326.5 | 192.1
FeSO4 | 329.0 | 180.6
MnSO4 | 208.6 | 108.6

## Slide 9: Measurement geometry

## Slide 10: Prompt gamma measurement
  Measurement of leakage gammas with HPGe and stilbene detectors
  Ideal geometry , Cf inside is standard, and large volume ensures ideal thermalization
  Aqueous solution → good moderation
  Plan to publish as SINBAD benchmark
Chart: E [keV]
Chart: E [MeV]
Energy range | Cl | Fe
0 - 1 eV | 97.738% | 99.404%
1 eV - 0.1 keV | 2.121% | 0.503%
0.1 keV - 10 keV | 0.134% | 0.053%
10 keV - 20 MeV | 0.007% | 0.039%

## Slide 11: Prompt gamma NaCl case
  Significant overprediction across libraries in NaCl case
  Cl is important in design of new reactors
  Importance in PGNAA issues
  Part of CRP (F40016 - Measurement of Prompt Capture Gamma Coming from Chlorine and Iron Neutron Capture )
Czakoj et al., Ann. Of Nucl. En., accepted manuscript

## Slide 12: Gamma spectra from solution – FeSO4
Chart: E [MeV]
Chart: E [MeV]
Chart: E [MeV]
HPGe calculation
Significant difference between libraries
Unphysical peaks especially in case of ENFB/VIII.0 a JEFF-4T2

## Slide 13: Gamma spectra from solution – FeSO4
E [MeV] | Measured flux [photon/cm2·s] | Measurement uncertainty | C/E-1 |  | C/E-1 uncertainty
 |  |  | JEFF-3.3 | JENDL-5 | 
3.186 | 1.21E-03 | 9.80% | -70.60% | missing | 10.30%
3.413 | 7.34E-04 | 36.00% | 28.80% | missing | 36.20%
3.437 | 1.13E-03 | 24.60% | -15.60% | missing | 24.80%
4.218 | 2.72E-03 | 11.10% | -5.70% | missing | 11.60%
4.406 | 8.56E-04 | 13.40% | 42.20% | - | 13.80%
4.810 | 2.69E-03 | 15.40% | -55.00% | - | 15.80%
5.920 | 6.94E-03 | 4.30% | 10.70% | -51.10% | 5.40%
6.019 | 8.06E-03 | 6.20% | -2.70% | -54.30% | 7.00%
7.279 | 4.89E-03 | 12.30% | 9.80% | 106.40% | 12.70%
7.631 | 2.55E-02 | 3.50% | 3.20% | -48.40% | 4.80%
7.646 | 2.13E-02 | 3.60% | 3.80% | -37.70% | 4.90%
8.886 | 9.92E-04 | 22.70% | -28.10% | - | 22.90%
9.298 | 3.12E-03 | 8.30% | 7.90% | -59.60% | 8.90%
Czakoj et al., Ann. Of Nucl. En., accepted manuscript
  Illustration of C/E-1 for selected peaks
  ENDF/B-VIII.0 not evaluated due to non physical peak shape

## Slide 14: 252Cf(s.f) TFGS spectrum measurement
The new measurement of Total Fission Gamma Spectra from 252Cf(s.f) source realized
„Only“ difference from neutron spectra measurement – Pb cone (instead of Fe-PE in neutrons )

## Slide 15: 252Cf(s.f) TFGS spectrum measurement
Room effect is very important, especially in higher energies
Must be evaluated experimentally – calculation disagree with experiment, especially in higher energies
Chart: E [MeV]
Chart: E [MeV]

## Slide 16: 252Cf(s.f) TFGS spectrum measurement
PSD discrimination – left part of spectrum – more simple than in neutron evaluation
Correction to structural component effect (cladding, flexo rabbit )
Chart: E [MeV]
| 0 | 15
1 | 1 | 1

## Slide 17: 252Cf(s.f) TFGS spectrum measurement
First measurement in region 0.1 – 14 MeV
Uncertainties
  7 – 10 % in 1 – 7 MeV
  Below 20 % in 7 – 9 MeV
  Up to 90 % in 14 MeV
Consistent with previous results
  Between Stoddard and Trykov results

## Slide 18: Gamma spectrum measurement in LR-0
Gamma spectrum measurement in special core (6 fuel assemblies) of 3.6% enrichment (2 years decay – very low background)
Chart: Energy [MeV]

## Slide 19: Gamma spectrum in LR-0
Measurement is consistent with ENDF/B-VIII.0
JEFF and JENDL show discrepancies in higher energies
Chart: Energy [MeV]
Chart: Energy [MeV]

## Slide 20: LR-0 experiments with heavy reflector
VVER-1000 Mock-Up for reactor dosimetry issues (now the focus is on internals (now it seems void swelling is at least a similar issue like embrittlement)
Flexibility allows to mix „Reference core“ & „VVER-1000 Mock-Up components“
Baffle full-scale simulator of VVER-1000 baffle of stainless steel 08Kh18N10T (18% Cr, 10% Ni, 1.5% Mn, residual Fe )
20

## Slide 21: The effect of iron – keff in various libraries
 | ENDF/B-VIII** | ENDF/B-VIII* | ENDF/B-VIII | ENDF/B-VII.1 | ENDF/B-VI.2 | JEFF-3.3 | JENDL-4
Case 1A | 1.00251 | 1.00111 | 1.00002 | 1.00075 | 0.99281 | 1.00107 | 1.00035
Case 1 | 1.00223 | 1.00096 | 0.99987 | 1.00072 | 0.99266 | 1.00092 | 1.00032
Case 2 | 1.00204 | 1.00063 | 0.99969 | 1.00032 | 0.99253 | 1.00083 | 1.00001
Case 3 | 1.00020 | 0.99893 | 0.99774 | 0.99838 | 0.99085 | 0.99895 | 0.99818
Case 4 | 1.00054 | 0.99920 | 0.99797 | 0.99873 | 0.99126 | 0.99931 | 0.99843
** The Fe was replaced by INDEN evaluation, O was replaced by ENDF/B-VII.1 evaluation
* The Fe was replaced by INDEN evaluation
The effect of steel was studied
Some discrepancies reported
However, steel has more components and „only“ some part is reflected
Kostal et al., The effect of heavy reflector on neutronic parameters of core, Ann. of Nucl. En., 168, (2022), 108898

## Slide 22: Validation of iron in reactivity experiments
The effect of iron on criticality was studied
Well validated flux and spectrum in central cavity + spatial distribution of fission + criticality
  Good for testing of inserted or side attached materials
    Steel (Iron + 1.5 % Mn)
Reference core . . . . . . . . . . 541.51 +/- 1.32 mm
Iron in center . . . . . . . . . . . . 579.01 +/- 0.79 mm
Iron around . . . . . . . . . . . . . 548.09 +/- 0.69 mm
Iron around + center . . . . . . . 598.23 +/- 0.92 mm
22

## Slide 23: Effect of iron on keff in various arrangements
 | ENDF/B-VIII.0** | ENDF/B-VIII.0* | ENDF/B-VIII.0 | ENDF/B-VII.1 | JEFF-3.3
12 + 1 | 0.99678 | 0.99546 | 0.99520 | 0.99538 | 0.99785
12 + 0 | 0.99809 | 0.99697 | 0.99651 | 0.99692 | 0.99946
0 + 1 | 0.99974 | 0.99821 | 0.99808 | 0.99843 | 1.00001
reference | 1.00091 | 0.99968 | 0.99960 | 0.99989 | 1.00176
** The Fe was replaced by INDEN evaluation, O was replaced by ENDF/B-VII.1 evaluation
* The Fe was replaced by INDEN evaluation
 | ENDF/B-VIII.0** | ENDF/B-VIII.0* | ENDF/B-VIII.0 | ENDF/B-VII.1 | JEFF-3.3
12 + 1 | 322 | 454 | 480 | 462 | 215
12 + 0 | 191 | 303 | 349 | 308 | 54
0 + 1 | 26 | 179 | 192 | 157 | 1
reference | 91 | 32 | 40 | 11 | 176
A reference neutron field has been identified in the driver core used
The experimentally determined water level is used in calculation
  ENDF/B/VIII.0 + various evaluation (Fe from INDEN, ENDF/B-VIII.1, O from ENDF/B-VII.1)
  Various libraries
  234U effect not evaluated yet – will be done (***) ( = positive bias ~ 100 – 150 pcm)
Part of APRENDE proposal – it is planned that the final evaluation will be benchmarked
*** Elyantev et al., Testing and Validation of Nuclear Fuel Composition Using SIMS Method, Journal of Nuclear Engineering and Radiation Science APRIL 2021, Vol. 7 / 022003-1
Difference from unity in pcm
keff calculated for defined experimental configuration
12+1
12+0
0+1
reference

## Slide 24: Development of new reference field
Mat. | Au | Cu | Fe | Mn | Au | Au | Au 1% | Ta | Au (Cd) | Cu (Cd) | Au 1% (Cd) | Au 1% (Cd) | Au 1% (Cd)
Pos. | S | S | S | S | A | B | B | C | C | C | S | A | B
1 | 0.0% | -9.6% | -8.9% | -5.2% | -2.8% | 1.0% | -3.8% | -5.7% | 12.6% | -11.6% | - | - | -
2 | 5.5% | -4.9% | -5.9% | -0.1% | 0.5% | 6.6% | 0.0% | 1.2% | 10.1% | -11.3% | - | - | -
3 | 5.2% | 0.1% | -0.9% | -1.0% | 3.1% | 4.3% | 0.5% | -0.3% | 4.1% | - | - | - | -
4 | 1.3% | -2.7% | 0.6% | -4.4% | 0.7% | 0.7% | -1.6% | 0.3% | -7.8% | - | -2.5% | -5.0% | -
5 | 0.9% | -6.1% | - | -7.9% | -2.2% | -0.7% | -6.1% | -6.3% | -12.6% | - | - | - | -10.6%
6 | -10.6% | -14.0% | -7.5% | -11.6% | -10.1% | - | - | -8.2% | -10.9% | -23.2% | - | - | -
7 | -17.0% | -21.1% | -16.6% | -18.0% | -18.6% | -14.0% | -19.3% | -3.9% | -15.7% | -31.9% | - | - | -
Characterization of channel (D=8 cm) in large graphite insertion
Good agreement in parts below water level (Hcr=39.13 cm)
Discrepancies in „dry graphite“ part

## Slide 25: Development of new reference field
Characterization of channel (D=8 cm) in „one channel“ graphite insertion (derived from current reference field)
Less thermalized than in previous case, but more sensitive !
Good agreement in parts below water level (Hcr=43.16 cm)
Discrepancies in „dry graphite“ part

## Slide 26: New experiments in benchmark reference neutron field
New experiments focused on validation of 14N(n,p) cross section
A very large set of reaction rates were evaluated
Chart: Energy [MeV]
14N(n,p)14C | Mean [b] | Unc. | C/E-1
Experiment | 0.3067 | 10.4% | -
ENDF/B-VIII.0 | 0.2920 | 0.10% | -4.8%
JEFF-3.3 | 0.2920 | 0.10% | -4.8%
JENDL-5 | 0.3060 | 0.10% | -0.2%

## Slide 27: New experiments in benchmark reference neutron field
Will be published in ANE

## Slide 28: Correction from LR-0 to 235U PFNS
SACS measured in LR-0 corrected to 235U PFNS are in good agreement (disagreement in 115In(n,n’) reflecting difference between LR-0 and 235U PFNS)
 | E50% | SACS [mb] | Rel. unc. | Eval./E-1
115In(n,n') | 2.589 | 209.3 | 2.70% | -10.30%
47Ti(n,p) | 3.647 | 17.97 | 2.00% | -0.70%
64Zn(n,p) | 4.036 | 38.21 | 5.30% | 1.80%
58Ni(n,p) | 4.051 | 106.1 | 2.20% | 2.00%
54Fe(n,p) | 4.294 | 78.33 | 2.40% | -0.30%
92Mo(n,p) | 5.19 | 6.938 | 2.20% | -3.60%
46Ti(n,p) | 5.862 | 10.72 | 2.20% | 7.40%
60Ni(n,p) | 6.811 | 2.086 | 8.50% | 4.50%
63Cu(n,α) | 7.019 | 0.5009 | 2.90% | 3.30%
54Fe(n,α) | 7.205 | 0.8707 | 10.50% | -0.70%
56Fe(n,p) | 7.362 | 1.05 | 2.60% | 2.80%
48Ti(n,p) | 8.103 | 0.2909 | 2.60% | 3.60%
24Mg(n,p) | 8.125 | 1.412 | 4.60% | 2.60%
27Al(n,α) | 8.471 | 0.6764 | 2.30% | 3.60%
51V(n,α) | 9.737 | 0.0234 | 3.50% | 4.00%
197Au(n,2n) | 10.414 | 3.372 | 4.00% | 0.40%
93Nb(n,2n)92* | 11.21 | 0.4307 | 3.10% | 0.90%
127I(n,2n) | 11.459 | 1.177 | 4.00% | 1.80%
55Mn(n,2n) | 12.796 | 0.2324 | 4.50% | 0.00%
75As(n,2n) | 12.797 | 0.3228 | 4.30% | -1.10%
89Y(n.2n) | 13.797 | 0.1698 | 3.20% | 0.80%
19F(n,2n) | 13.911 | 0.00769 | 4.00% | 5.90%
90Zr(n,2n) | 14.32 | 0.1053 | 4.00% | -0.70%
23Na(n,2n) | 15.483 | 0.00394 | 4.80% | -1.90%

## Slide 29: 58Ni(n,x)57Co validation in 235U PFNS
High threshold reaction low sensitive for gamma
New measurements performed in LR-0 reference field - identity with 235U PFNS > 6 MeV
Previous measurements were realized in VR-1 reactor (CTU university reactor with known neutron field - identity with 235U PFNS > 6 MeV < 12 MeV)
Good agreement across measured set of SACS
Reference | Mean [mb] | Difference from current value
BRUGGEMAN et al., 1974 | 0.216 ± 0.005 | -7.1%
WÖLFLE et al., 1980 | 0.240 ± 0.035 | 3.2%
HORIBE et al., 1992 | 0.232 ± 0.005 | -0.2%
ZAIDI et al., 1993 | 0.253 ± 0.015 | 8.8%
Arribére et al., 2001 | 0.275 ± 0.015 | 18.3%
Burianova et al., 2019 | 0.239 ± 0.013 | 2.8%
Kostal et al 2021 | 0.241 ± 0.015 | 3.7%
Kostal et al 2022 | 0.226 ± 0.009 | -2.9%
2023 measurement in LR-0 | 0.233 ± 0.014 | 
Chart: E [MeV]
 | 0 | 0
VR-1 spectrum validation

## Slide 30: Measurements in medical accelerators
UJV (parent company of CV Rez) operating 3 IBA cyclotrons – one of them is in Rez
Large set of measurements was realized
Now - IAEA CRP on leakage spectra
Chart: Energy [MeV]
Kostal et al, NIMA, 942, (2019), 162374

## Slide 31: Measurements in cyclotron background
In back-scattered neutrons significant discrepancies observed
The measurement is reliable, as is consistent with experiment in cyclotron U-120M in Rez
Systematic shift FENDL-3 v.s experiment
Zmeskal et al, ARI, 199 (2023) 110865
Hagiwara M. et al., Measurement of Neutrons and Gamma-Rays from Thick H182O Target Bombarded with 18 MeV Protons. JKPS 2011;59:2035-2038

## Slide 32: Measurements on target
Very large set of RR measurement performed (during routine production
Large discrepancies in higher energy threshold reactions
Use of new reaction 58Ni(n,x)57Co
MCNP 6.2 is slightly better than previous MCNP 6.1but ….
Kostal et al., Rad. Phys. and Chem., 184 (2021) 109475
nat.Ni(n,x)58Co / nat.Ni(n,x)57Co

## Slide 33: Characterization of compact generators
Czakoj et al., NIMA., 1034, (2022), p. 166837
Kostal et al, Ann. of Nucl. En., 191, (2023), p. 109904
  Characterization of spectra (opposite geometry than assumed)
  Characterization of lower peaks flux by 115In(n,n’)
  Used in measurement of dosimetry cross sections

## Slide 34: Characterization of Rez D-T generator
Czakoj et al., NIMA., 1034, (2022), p. 166837
  Usable for integral experiments
  The voltage drives especially the neutron emission (increasing cross sections)
  Some slight energy broadening observed in energy of main peak when voltage shift from 55 to 95 keV.

## Slide 35: Conclusions
New benchmarks become part of ICSBEP database
High energy gamma is issue. The methodology developed in Rez (using solution and point source) is suitable for validation of gamma production – the benchmarking will follow
New measurement of TFGS from 252Cf(s.f) source was realized
New measurement of special core was realized. The ENDF/B-VIII.0 evaluation of 235U PFGS seems to be closer to experiment than other evaluations
Validation of iron effect on criticality realized still some discrepancies persists

## Slide 36: Thank you for attention
Michal Kostal
Michal.Kostal@cvrez.cz

## Slide 37: Future plans (Al leakage experiment)