## Slide 1
PIGE in NDF: implementation and round robin results
Nuno P. Barradas
nunoni@ctn.tecnico.ulisboa.pt, N.Pessoa-Barradas@iaea.org
On leave from Centro de Ciências e Tecnologias Nucleares, Instituto Superior Técnico, Universidade de Lisboa
Presently at the International Atomic Energy Agency. The views expressed do not reflect those of the IAEA or its Member States.

## Slide 2: Overview
Basic principles of PIGE calculation from first principles
Implementation
  Handling of stopping power
  Handling of cross sections
  Definition of sub-layers
NDF code
  Basic data
  Language etc
  Input and output
IAEA intercomparison of PIGE codes
  Some results
  Final comments

## Slide 3: Basic principles of PIGE simulation
Divide sample into sub-layers
Calculate incident energy on each layer: energy loss
Calculate cross section on each layer: from tabulated cross section
Assume no absorption of g rays
Integrate yield over all layers
Points to consider:
  In a sub-layer, do we take the cross section on top or bottom of layer, or something else (integrate over sub-layer)?
  In a sub-layer, do we calculate energy loss with the stopping power at top of the layer, or something else (integrate over sub-layer)?
  Straggling can have strong effect in multilayered samples

## Slide 4: Implementation: Stopping power (1)
In NDF, any combination of sources of stopping powers can be used:
  Tabulated (i.e. experimental ):
    For elements
    For molecules (e.g. SiO2)
  Calculated:
    ZBL95
    ZBL2000
    SRIM: used in this case
    MSTAR
SRIM: called at first use of a given ion in a given element in a given energy range
  Produces a file with 5000 stopping values calculated for equally spaced energy values
  If same ion/element/energy range needed again, and version of SRIM did not change, then file is read
  Linear interpolation made on tabulated values

## Slide 5: Implementation: Stopping power (2)
In a sub-layer:
  If energy loss in sub-layer smaller than ½ the energy step in internal table, take the stopping power at top of the layer
  Otherwise integrate over sub-layer (3- or 5-point Simpson)
Because stopping power changes slowly, this is accurate enough, as long as sub-layer not enormously thick

## Slide 6: Implementation: Energy spread
In-built models: Bohr, Chu, Tschälär
WDEPTH: used to calculate Doppler (0.1 keV)
Doppler added in quadrature with FWHM
Energy spread shape: Gaussian or gamma function (inspiration from Matej’s paper on roughness)
Options taken
  “Gaussian”: Bohr straggling, no Tschälär, Doppler=0.1 keV, Gaussian
  “Full”: Chu+Tschälär, Doppler=0.1 keV, gamma function

## Slide 7: Implementation: Cross section (1)
Three issues:
  Initial yield is user input
  Integration within each sub-layer essential whenever cross section changes faster than sub-layer energy width
  Convolution with energy spread essential in layered targets, where (real) layer energy width comparable to resonance width
NDF integrates experimental cross sections over each sub-layer

## Slide 8: Implementation: Cross section (2)
NDF integrates cross section over energy spread
  Yield can change dramatically for thin layers
  In bulk targets, shape can change as well
Example for p-RBS:
1 mm Mylar film under a 4.2 mm Ni film
Three issues:
  Initial yield is user input
  Integration within each sub-layer essential whenever cross section changes faster than sub-layer energy width
  Convolution with energy spread essential in layered targets, where (real) layer energy width comparable to resonance width

## Slide 9: Implementation: Definition of layers
Usually following method for sub-division of layers is used:
  User defines internal layer thickness for 1.5 MeV 4He RBS (default: 50x1015 at/cm2)
  NDF scales to actual problem by scaling to stopping powers
  Maximum and minimum imposed. In this case, not needed
Whenever cross section is not Rutherford (i.e. RBS and ERDA), and a file is input:
  Autolayer: Create further sub-layers, by creating extra division points at all energies where a cross section value is given
  In present case, little difference towards simple sub-division

## Slide 10: Code: Basic data
Navogadro=6.022140857e23
pi=3.141592654
e_charge=1.6021766208e-19
e0_permitivity=8.854187817e-12
c following are in kg
p_mass=1.672621898e-27
n_mass=1.674927471e-27
e_mass=9.10938356e-31
c following is in amu
e_mass_u=5.485799090e-4
Isotopic masses and natural abundances: 27Al 100%.
NDF uses single precision (compil: extended precision) except in critical routines

## Slide 11: Code: Language etc
NDF is written in Fortran (insert version here: whatever is available in compiler):
  Compiler: Digital/Microsoft
  Possibly some very few compiler extensions are used; none on actual calculations
  No libraries used
  PIXE routine is in C, compiled as object with Fortran/C interface
Described in Status of IBA data analysis and simulation software, E. Rauhala et al., Nucl. Instrum. Methods Phys. Res. B244 (2006) 436-456
Took part in International Atomic Energy Agency intercomparison of Ion Beam Analysis software, N.P. Barradas et al., Nucl. Instrum. Methods Phys. Res. B262 (2007) 281-303.
Took part in International Atomic Energy Agency intercomparison of Ion Beam Analysis software, N.P. Barradas et al., Nucl. Instrum. Methods Phys. Res. B 468 (2020) 37-47
Proprietary, commercial, general purpose, in active (currently slow) development
PIGE routine partly open source, input data including stopping power and cross sections come from NDF

## Slide 12: Code: Input and output
Input
  (basic data)
  (NDF stuff: license, config file, etc)
  “Experimental” data: table of Energy/Yield
    Calculation is made independently, consecutively, for each energy in table
  Depth profile to be calculated
  Experimental conditions
  Calculation options
Output
  Calculation: table with Energy/Experimental yield/Calculated yield
  Result file with all calculations made, options, depth profile, etc
  (assorted files with extra information, including intermediary calculations etc)

## Slide 13: Intercomparison: Autolayer
Calculations for automatic further subdivision of layers at each energy given in the cross section file (autolayer)
Up to 1 part in 100000 difference. Autolayer on more stable: hence reported values used autolayer on

## Slide 14: Intercomparison: NDF vs SPACES, calc 2 (1)
Used apps.automeris.io/wpd to extract numerical data. Not fully accurate (depends on manual input of 2 x and 2 y reference data points)
Normalized SPACES to NDF
It seems like NDF fairly reproduces SPACES, with a shift in the Lewis peak for 1 keV
But… let’s calculate with 50 eV steps

## Slide 15: Intercomparison: NDF vs SPACES, calc 2 (2)
NDF overestimates the Lewis peak: gamma function not realistic at very small energy losses

## Slide 16: Intercomparison: NDF vs SPACES, calc 2 (3)
Not a new result! This limitation in the NDF model is already known since 2010
C: stronger straggling, lower stopping, hence much stronger Lewis effect

## Slide 17: Intercomparison: calc 7 (1)
All three codes agree extremely well for Gaussian straggling
NDF significantly different for full straggling:
  Curves for ERYA-Prof and SIMNRA are nearly identical with Gaussian and full straggling. This is unexpected since “Gaussian” was defined as “Bohr, no Tschälär”, while “Full” was “best model” (for NDF, Chu+Tschälär+Doppler)
Chart: Ex 7 ΔE=0
| 2000 | 2002 | 2004 | 2006 | 2008 | 2010 | 2012 | 2014 | 2016 | 2018 | 2020 | 2022 | 2024 | 2026 | 2028 | 2030 | 2032 | 2034 | 2036 | 2038 | 2040
ERYA | 4.5266 | 4.7089 | 4.8449 | 4.9299 | 4.9622 | 4.94 | 4.8657 | 4.7417 | 4.5735 | 4.3675 | 4.1318 | 3.8741 | 3.6044 | 3.3313 | 3.0658 | 2.8155 | 2.5903 | 2.3955 | 2.2398 | 2.1254 | 2.0567
NDF | 4.5525 | 4.7277 | 4.8557 | 4.9326 | 4.9561 | 4.926 | 4.8437 | 4.7131 | 4.5387 | 4.3279 | 4.0886 | 3.8289 | 3.5587 | 3.2869 | 3.0233 | 2.7772 | 2.5561 | 2.3677 | 2.218 | 2.1114 | 2.0507
SMNRA | 4.4376 | 4.5973 | 4.7138 | 4.7838 | 4.8055 | 4.7788 | 4.7051 | 4.5877 | 4.4313 | 4.2417 | 4.0259 | 3.7918 | 3.5479 | 3.3027 | 3.0646 | 2.8417 | 2.6414 | 2.4703 | 2.3338 | 2.2356 | 2.1784
Chart: Ex 7 Full ΔE=0
| 2000 | 2002 | 2004 | 2006 | 2008 | 2010 | 2012 | 2014 | 2016 | 2018 | 2020 | 2022 | 2024 | 2026 | 2028 | 2030 | 2032 | 2034 | 2036 | 2038 | 2040
ERYA | 4.4567 | 4.6648 | 4.828 | 4.9416 | 5.0024 | 5.009 | 4.962 | 4.8638 | 4.7186 | 4.532 | 4.3111 | 4.064 | 3.7996 | 3.5271 | 3.2562 | 2.9963 | 2.7562 | 2.544 | 2.3668 | 2.2302 | 2.1383
NDF | 4.1174 | 4.2299 | 4.3091 | 4.3535 | 4.3625 | 4.3372 | 4.2792 | 4.1915 | 4.0776 | 3.9418 | 3.7896 | 3.6259 | 3.4572 | 3.2889 | 3.127 | 2.9771 | 2.8435 | 2.7302 | 2.6409 | 2.5779 | 2.5418
SMNRA | 4.3473 | 4.5405 | 4.6899 | 4.791 | 4.8437 | 4.8477 | 4.8025 | 4.7092 | 4.5736 | 4.401 | 4.1959 | 3.9646 | 3.7172 | 3.4626 | 3.2099 | 2.9685 | 2.7465 | 2.5507 | 2.3875 | 2.2614 | 2.1763

## Slide 18: Intercomparison: calc 7 (2)
First step: look at, for e.g. 2000 and 2040 keV beam energy:
  Energy before scattering
  FWHM for Gaussian (i.e. Bohr) and full (i.e. Chu+Tschälär)
  (Gaussian vs. gamma does not play a role, results are nearly identical)

## Slide 19: Intercomparison: calc 7 (3)

## Slide 20: Intercomparison: calc 7 (4)

## Slide 21: Intercomparison: calc 7 (5)
Nuno’s personal conclusions:
  NDF results follow what is expected from the assumptions taken on what “Gaussian” and “full” mean.
  ERYA and SIMNRA: for similar assumptions, results would seem to be wrong. Question: what were in fact the assumptions?

## Slide 22: Intercomparison: Some final comments
NDF results depend for some of the calculations on the integration step: too large and they deviate.
  Current integration step comes from a built-in universal parameter for all techniques in NDF: 50x1015 at/cm2 for 1.5 MeV in Si 4He-RBS; normalized to stopping power ratio for other cases
  It can be changed by the user (within the ranges 0.1 and 1000 x1015 at/cm2 )
  Values below 50 down to about 10 (did not try lower): stable calculation
  Values above 100-200: deviations observed

## Slide 23
Thank you!